ABSTRAK

Barium karbonat sering digunakan sebagai energizer pada proses kotak karburisasi padat, namun penggunaan barium karbonat memiliki beberapa keterbatasan selain harganya yang mahal, barium karbonat juga tidak ramah lingkungan dan merupakan zat kimia yang berbahaya, sebagai energizer pada proses kotak karburisasi dapat digunakan kalsium karbonat yang terdapat pada cangkang keong emas yang mudah di temukan disekitar kita. Tujuan dari penelitian ini adalah untuk mengetahui pengaruh penambahan serbuk cangkang keong emas pada proses kotak karburisasi terhadap sifat fisis (uji komposisi dan foto struktur mikro) dan mekanis (uji kekerasan) baja karbon rendah setelah mengalami perlakuan.

Bahan yang digunakan dalam penelitian ini adalah baja karbon rendah yang berbentuk selinder. Proses pembuatan spesimen dilakukan dengan pemotongan menjadi beberapa bagian, pemotongan dilakukan untuk memudahkan di dalam meletakan spesimen di dalam kotak karburisasi,kemudian serbuk arang kayu dan serbuk cangkang ditimbang sesuai dengan komposisi yang diinginkan dengan pencampuran serbuk cangkang 5, 10 dan 15 (% berat).Setelah dibuat benda uji, dilakukan perlakuan panas pada temperatur 9500C dengan penahanan waktu selama 2, 4 dan 6 (jam). Kemudian dilakukan Uji kekerasan Vickers,  pengujian foto struktur mikro dan uji komposisi.

Dari hasil penelitian menunjukkan bahwa pada penambahan serbuk cangkang keong emas 5, 10 dan 15 (% berat) pada baja karbon rendah setelah mengalami perlakuan diperoleh nilai kekerasan tertinggi rata-rata pada penambahan 15% serbuk cangkang di peroleh sebesar 262,26 kg/mm2 dan kekerasan material awal diperoleh sebesar 144,08 kg/mm2. Dari hasil pengamatan struktur mikro dan uji komposisi diketahui bahwa terjadi pengerasan permukaan karena difusi karbon kedalam baja karbon randah.

Kata Kunci : Cangkang keong emas, Energizer, Karburisasi padat, Baja karbon rendah

ABSTRACT 

                 Barium carbonate is often used as an energizer in the process of pack carburizing , but the use of barium carbonate has several limitations in addition to its price, barium carbonate is also not environmentally friendly and is a dangerous chemical substances, as an energizer in the process of carburization box can be used calcium carbonate contained in the Pomacea Canalikulata Lamarck found easily on around us. The purpose of this study was to investigate the effect of Pomacea Canalikulata Lamarck powder addition on the process of carburization box to physical properties (test composition and microstructure images) and mechanical (testing hardness) of low carbon steel after heat treatment. 
                  Materials used in this research is a form of low carbon steel cylinder. The process of making the specimen is done by cutting into several pieces, cutting done to ease in placing the specimen in the carburizing box, then wood charcoal powder and shell powder were weighed in accordance with the desired composition by mixing powder and 15 shells of 5. 10 (wt%). Having made the test piece performed at a temperature of 9500C heat treatment with the holding time 2, 4 and 6 (h). Then, the Vickers hardness test,

microstructure and test photo composition  test.

The result showed that the addition of 5.10 Pomacea Canalikulata Lamarck powder and 15 (wt%) on low carbon steel after being subjected to the highest hardness value obtained on average at 15% addition of shell powder was obtained at 262.26 kg/mm2 and initial material hardness was obtained at 144.08 kg/mm2. From microstructure observation and composition test is known that there is carbon diffusion surface hardening because low into carbon steel

Keywords: Pomacea Canalikulata Lamarck, Energizer, pack carburizing, low carbon

steel